## Slide 1: A radiation-induced nanostructure evolution model for Fe-C, Fe-C-Cr and other alloys
V. Jansson, M. Chiapetto, L. Malerba
(coll. D. Terentyev, N. Castin, N. Anento*, A. Serra*)
Structural Materials: Modelling and Microstructure
Institute of Nuclear Materials Science – SCK•CEN
Boeretang 200 – 2400 Mol (Belgium)
lmalerba@sckcen.be
*Universidad Politécnica de Catalunya, Barcelona, Spain

## Slide 2: What did we do
Combined all information available from experiments and atomistic simulations to describe quantiatively the properties of radiation defects in Fe
Rationalised the effect of C on nanostructure evolution under irradiation in Fe based also on review of experiments and ad-hoc simulations
Developed a physics-based model that describes satisfactorily the nanostructure evolution under irradiation in Fe-C under a variety of conditions
Added to Fe-C the effect of Cr (in 1st approximation)

## Slide 3: Key process: Carbon-vacancy complexes trap loops
complex | Eb<111> (eV) /Em<111>~0.05 eV | Eb<100> (eV) /Em<100>~1 eV
C | 0.6-0.7 (edge) | 1.0 (edge)
C-V | 0.75 (edge) | n.c.
C-V2 | 1.4 (centre) / 0.6 (edge) | n.c.
C2-V | 1.5 (edge) | 0.6 (edge)
N. Anento, A. Serra, J. Nucl. Mater., accepted
This process allows 50 yrs of irradiation experiments on Fe-C alloys and mild steels to be rationalised

## Slide 4: Parameters for effect of C
C and C2-V complexes are dominant traps for SIA clusters at 300°C (C-V2 at <100°C)
They are modelled as immobile traps
Mainly <100> loops observed experimentally at Tirr=300°C 
At <100°C only <111> loops observed  all of this type
Assumptions
Invisible loops are a mixture of <111> & <100>
  Mig. energy ~0.2 eV
  Trapping energy ~111
Visible loops <100>
  Mig. energy ~0.9 eV
  Trapping energy ~100
Key assumption
When loops are small interaction occurs with edge and is weaker

## Slide 5: Tirr < 100°C

## Slide 6: Vacancy clusters vs dpa
Fe ~100 appm C
Irradiation in HFIR @ 70°C & ~10-8 dpa/s up to ~0.8 dpa
Zinkle & Singh, J. Nucl. Mater. 351 (2006) 269
Good reproduction of density, with slight underestimation of size
Threshold for loop/CV2 interaction with centre is ~30 SIA (< 1 nm )
Notes: 6

## Slide 7
Fe ~100 appm C
Irradiation in HFIR @ 70°C & ~10-8 dpa/s up to ~0.8 dpa
Zinkle & Singh, J. Nucl. Mater. 351 (2006) 269
Visible SIA cluster density vs dpa
Reasonable reproduction of density vs dose (except very low dose, because in reality traps are not there yet!), with slight overestimation of size
Threshold for loop/CV2 interaction with centre is ~30 SIA (< 1 nm )
Notes: 7

## Slide 8: Tirr ~ 300°C

## Slide 9
Fe ~100 appm C
Irradiation in BR2 @ 290°C & ~10-7 dpa/s up to ~0.2 dpa
REVE Experiment
Vacancy cluster density/size vs dpa
PAS 
~12 vacs
~1023 m-3
SANS
~2 nm
41022 m-3
Good results for density and size of vacancy clusters vs experimental data
(slight overstimation of size, underestimation of density)
Low T data for comparison
Notes: 9

## Slide 10
Fe ~100 appm C
Irradiation in BR2 @ 290°C & ~10-7 dpa/s up to ~0.2 dpa
REVE Experiment
SIA cluster density/size vs dpa
Reasonable reproduction of density and size of SIA
clusters vs experimental data.
Slight overestimation of density and underestimation of size
Notes: 10

## Slide 11: Limitations and Perspectives
Limitations
Difficulty of unknown details of the process of formation of <100> vs <111> loops
Assumption of immobile traps instead of C atoms forming complexes
Perspectives
Introduce explicit treatment of mobile C atoms
Explore assumptions about <100> vs <111>

## Slide 12: Model for Fe(-C)-”Cr”

## Slide 13
%Cr | Grain size | Dislocation density (1013m-2) | wt%C
2.5 | 50 | 1.2 | 0.01
5 | 35 | 5.8 | 0.02
9 | 20 | 6.3 | 0.02
12 | 15 | 5.5 | 0.03
Fe-Cr: Irradiation in BR2 @ 290°C & ~10-7 dpa/s up to ~0.06 dpa
MIRE-Cr Experiment
%Cr | SIA cluster mean size (nm) | SIA cluster density (1021 m-3)
2.5 | 8/4* | 1.2 /0.5*
5 | 7 | 1.4
9 | 6/4* | 1.3 /0.08*
12 | - | -
*M. Mayoral
PAS

## Slide 14: Assumptions to simulate Cr effects
Self-interstitial clusters are slowed down by Cr atoms non-monotonically with Cr content / the effect disappears with increasing size

## Slide 15: Assumptions to simulate Cr effects
Visible loops are mainly of <111> type in Fe-Cr >2.5%Cr
C segregated to grain boundaries (lath boundaries) in alloys with martensitic structure (>2.5%Cr)
  50 appm in the matrix
  20 appm in the matrix
Vacancy size distribution for 5 %Cr (C = 50 appm) at 0.06 dpa

## Slide 16: SIA clusters
2.5%Cr (100 appm C) | 9%Cr (50 appm C) | 9%Cr (20 appm C)

## Slide 17: Limitations and Perspectives
Limitations
Difficulty of introducing full microchemical details: first approximation models
Smallness of the box to get statistics on visible loops
Perspectives
Take into account in more explicit way, possibly with the help of neural networks, the effect of Cr on defects and defect clusters
Explore assumptions about <100> vs <111>

## Slide 18: Model for Fe(-C)-”MnNi”

## Slide 19: Assumptions to simulate Mn & Ni effects in OKMC model
Vacancies are slowed down significantly by Mn (and Ni), effective migration energy on the order of ~1 eV
Self-interstitial clusters interact so strongly with Mn (and Ni) that they become virtually immobile above a relatively small size (~6-7 SIA)
(These are limiting cases: extreme assumptions!
But are “educated guesses” from DFT studies)

## Slide 20: Results of adding the “effect of Mn (Ni)”
Reduced mobility of vacancy clusters leads spontaneously to absence of voids (no coalescence)
Only single & di-vacancies
Fe”MnNi”
FeC
Vacancy clusters

## Slide 21: Results of adding the “effect of Mn (Ni)”
M. Hernandez-Mayoral, D. Gomez-Briceno, J. Nucl. Mater. 399 (2010) 146.
FeNiMn
Fe-C
Visible interstitial dislocation loops
FeNiMn
Fe-C

## Slide 22: Results of adding the “effect of Mn (Ni)”
INvisible interstitial dislocation loops
Mean size of all from OKMC
~3 nm 
Mean size of TEM visible ones
Density of invisible loops vs dpa
Density of ~1.5 nm  MnNi clusters according to APT
M. Hernandez-Mayoral, D. Gomez-Briceno, J. Nucl. Mater. 399 (2010) 146.
E. Meslin, B. Radiguet, P. Pareige, A. Barbu, Journal of Nuclear Materials 399 (2010) 137
LBPs might be SDLs, solute decorated loops!

## Slide 23: Limitations and Perspectives
Limitations
Difficulty of introducing full microchemical details: first approximation models
Smallness of the box to get statistics on visible loops
Perspectives
Develop simple model including explicitly Mn & Ni (at least), including their transport by single point-defects

## Slide 24: Summary
Main effect of C in the matrix is that it forms highly stable small complexes with vacancies
These complexes in turn trap mobile loops
Simple assumptions on the effect of Cr on mobility and types of SIA clusters + absence of C in the matrix provide correct trend of swelling vs Cr content
Two simple, though drastic, assumptions on Mn&Ni effect on SIA and V clusters devolve experimental nanostructure for FeMnNi alloys
Main conclusion: mobility of defects matters!

## Slide 25: Thank you for your attention!