## Slide 1
Modeling of diffusion, segregation and decomposition of alloys using OKMC: Applications to FeCr
Ignacio Martin-Bragado1, Ignacio Dopico1 and Pedro Castrillo2
1 IMDEA Materials Institute, Getafe, Spain
2 Department of Electronics, University of Valladolid, Spain

## Slide 2: Why FeCr alloys?
FeCr steels are the materials of choice for high temperature applications under irradiation.
An approximation to such steels is having a modeling framework for the FeCr alloy
Swelling in FeCr alloys under irradiation is around one order of magnitude lower than in pure Fe for the same dose.
Motivation

## Slide 3: Why atomistic simulations?
Requirements for FeCr alloy simulation:
Large periods of time (where MD is too short!)
Relatively big systems (where Lattice KMC is too memory consuming).
Including damage irradiation (from BCA or MD)
Predictive (useful: link to ab-initio).
Possible solution: off-lattice OKMC with quasi-atomistic FeCr spinodal decomposition model.
Motivation

## Slide 4: Previous work: SiGe alloys
Recent experience: Atomistic modeling and OKMC simulation of diffusion in SiGe alloys
Motivation
Castrillo et al, J. Appl. Phys. (2011)
Powerful approach, suitable for FeCr

## Slide 5: Goals
The goal it to develop a non-lattice, object KMC model for FeCr alloys able to:
  Simulate realistic times and sizes.
  Be integrated in a comprehensive OKMC simulator including other radiation effects.
  Reproduce and explain interdiffusion and separation.
  Include the effects of excess point defects.
This work

## Slide 6: Outline
Modeling of diffusion, segregation and decomposition of alloys using OKMC: Applications to FeCr
Atomistic model
Code implementation
Simulation results
Conclusions
This work

## Slide 7: Diffusion in binary alloys
Mobile point defects  defect diffusion → (K = V, I)
Atom diffusion driven by V or I → (A = Fe, Cr)
Interdiffusion driven by V or I →  concentration modification
Fe
Cr
Fe
Cr
I
V
I
V
Defect diffusion
V
I
Atom diffusion
Inter-diffusion
Fe
Cr
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→
Atomistic Model

## Slide 8: Point defect diffusion
Defect diffusivity
Point defect fluxes depend on DKCK.
In metals in equilibrium, CI << CV  DICI << DVCV
Both CI and CV enhanced with radiation damage (so, I’s could also play a role)
Atomistic Model
I
V
I
V
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 9: Point defect jumps
Defect generation: thermal (→ ) and radiation damage
Random walks with (migration →)
and depend on alloy composition
Energy jump barriers →
Atomistic model
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 10: Atom diffusion
Atomistic model
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→
In homogeneous alloys (no energy change): “tracer” diffusion
In general, .
Fitted to experiments.
Warning: “bulk” diffusivities, no dislocation-mediated ones, are relevant in the nanoscale.
Ab-initio calculations could be also a choice as an input for our model
Cfr. Martinez et al, PRB 2012

## Slide 11: Atom movements
Defect movement  atom movement (I →, V ←)
The probability of moving Cr or Fe depends on:
  The Cr and Fe content (configurational entropy)
  The diffusivity ratio
  The total energy modifications of the system: different final state after moving a Fe or a Cr
Atomistic model
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 12: Energy modifications
Energy changes: - mixing enthalpy
  - elastic energy release.
  Minimized for homogenous alloy
   is low in FeCr ,  0.45% ( but up to 4.2% in SiGe)
Atomistic model
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 13: Energy modifications (II)
Atomistic model
Different energy modification when an atom moves from a region 1 to a region 2 in Fe1-xCrx:
This affects the relative rates of Cr and Fe atoms moving from 1 to 2 :
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 14: Interdiffusion
Composition modification in inhomogeneous alloy.
For no net atom flux ():
Interdiffusion coefficient ():
 homogenization (as usual).
 separation (notably for Fe1-xCrx at low T)
Atomistic model
Fe1-xCrx
Fe1-yCry
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 15: Interdiffusion coefficient
Analytic results
for Fe1-xCrx is analytically derived to be:
  Nernst-Planck equation.
  Φ is the “thermodynamic factor” (see later).
  For x~0.5, is limited by the slowest diffuser.
  Valid in the nanoscale: defect mean free path.
Total interdiffusion coefficient:
is enhanced with radiation-induced defects:
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 16: Thermodynamic factor
Analytic results
The “thermodynamic factor” Φ is found to be:
In FeCr, the strain term can be neglected. (In contrast, in SiGe the two terms had opposite sign and almost compensate)
mixing
strain
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 17: Spinodal decomposition
Analytic results
Spinodal decomposition
Tsp(x)
If spinodal decomposition
This happens if for with:
Also found from
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 18: Miscibility gap
Analytic results
Miscibility gap
Tmg(x)
Phase diagram
Tsp(x)
Regions 1 and 2 have null interdiffusion flux if:
Miscibility gap edge for:
Also found from
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→
Notes: In our model, two neighboring regions 1 and 2 have interdiffusion flux if:

## Slide 19: The FeCr phase diagram
Malerba at al, JNM 2008
Miscibility gap
DEFECTS
INTERDIFF.
THERMODYN.
DECOMPOSITION
ATOMS
ENERGIES
→
→
→
→
→

## Slide 20: Object Kinetic Monte Carlo
Implemented in MMonCa code.
using the Object Kinetic Monte Carlo (non-lattice) approach.
Simulation sizes up to ~500 nm.
Simulation driven by events: times from s to years, depending on event rates.
Very suitable for damage evolution simulation.
Code implementation

## Slide 21: Quasi-atomistic approach
  Atomistic handling of defects: particles
  Continuum handling of the crystal: boxes
  Quasi-atomistic handling of alloy composition: Cr atom counters
  Particle properties depend on alloy composition in the box
  Jump probability rejection as a function of (Eform+Em)
Code implementation
1
2

## Slide 22: Composition evolution
Simulated composition histograms after annealing at 600K, starting at 
Simulation results
no separation
nucleation
nucleation-spinodal decomposition
spinodal decomposition
nucleation-spinodal decomposition
nucleation
no separation
occurrence

## Slide 23: Miscibility gap
alloy composition, x
Temperature (K)
Final composition at different temperatures
Color histograms. Initial composition: x = 0.5.
Simulation results
miscibility
G minima (miscibility curve) populated at each T

## Slide 24: Nucleation and growth
Simulated view of evolution for Tsp(x) < T < Tmg(x) (x = 0.05, 100ºC, 50 nm x 50 nm x 8 nm)
Simulation results
Nucleation and growth

## Slide 25: Spinodal decomposition
Simulation results
Homogeneous, spinodal decomposition
Computation time: 2h, 1 core.
Simulated view of evolution within the spinodal decomposition range (x = 0.5, 350ºC, 100nm x 100nm x 8 nm)

## Slide 26: Summary
An efficient off-lattice OKMC model for phase separation in FeCr has been presented.
Analytical expressions to assist in understanding the results have been shown.
Part of the FeCr phase diagram is reproduced.
Results showing nucleation and growth and spinodal decomposition and have been presented.
The model is integrated in a full OKMC simulator of damage irradiation evolution.
Conclusions

## Slide 27: Future work
Adjust the mixing enthalpy to better reproduce the experimental phase diagram.
Diffusivities and time-scale validation.
Study and calibrate the effects produced by excess of point defects generated by irradiation.
Finish the full integration into the simulator by including dependencies on Cr concentration to all the simulated defects (clusters, bubbles, …)
Conclusions

## Slide 28
THANK YOU VERY MUCH FOR YOUR ATTENTION