## Slide 1: Characterization of He implanted Eurofer97
Inês Carvalho, Henk Schut, Alexander Fedorov,
Natalia Luzginova, Pierre Desgardin, Jilt Sietsma
Edinburgh, 4-5 June 2013

## Slide 2: Outline
Project overview
Techniques
    Positron annihilation
    Thermal desorption spectroscopy
Experimental details
Results
    Helium implantations - 500 keV and 2 MeV
    Helium release mechanisms
      Example: 500 keV, 1016 He/cm2
      Overall picture
Final remarks & Future Work

## Slide 3: Project Overview
      Eurofer97 (Fe - 9Cr - 1W - 0.2V - 0.1Ta - 0.1C wt.%)
      Correlation of microstructure and mechanical properties
          Understanding structural defects that affect the mechanical properties
          Evolution of defect structures formed due to clustering and coalescence of POINT DEFECTS
              Helium-vacancy clusters
              Helium-filled bubbles
              Interstitial loops
      Thermal desorption spectroscopy (TDS)
        defect populations
        thermal stabilities of defects
      Positron annihilation
        thermal evolution of free-volume related defects
      Electron Microscopy
        microstructure of ion implanted and (neutron) irradiated samples

## Slide 4: Project Overview
      Use of thermal desorption spectroscopy (TDS) and electron microscopy on Eurofer97 neutron irradiated material
      First approach: reproduction of neutron irradiation conditions
          He implantation with 500 keV and 2 MeV energies
          Study of defect structures by positron annihilation and Thermal Desorption Spectroscopy (TDS)
        After: comparison of results – He implanted vs. neutron irradiated samples
Reference Material
Study of pre-existing defects
Ion Implantation (He)
Simulation of neutron irradiation defects
Neutron Irradiation
Real irradiation conditions
now

## Slide 5: Techniques

## Slide 6
Techniques – VEP
Positron annihilation
Variable energy positron beam (VEP)
22Na source
Energy up to 25 keV (~ 1µm depth for Fe)
Thermalization followed by trapping and annihilation
Emission of 2of 511 keV
Lifetime of 200 ps
W parameter  core electrons
S parameter  free electrons
 vacancies,
dislocations,
free volumes

## Slide 7
Techniques – VEP
Positron annihilation
Variable energy positron beam (VEP)
22Na source
Energy up to 25 keV (~ 1µm depth for Fe)
Thermalization followed by trapping and annihilation
Emission of 2of 511 keV
Lifetime of 200 ps
W parameter  core electrons
S parameter  free electrons
 vacancies,
dislocations,
free volumes

## Slide 8
Techniques - TDS
Thermal desorption spectroscopy
Heating rate of 0,33 K/sec
Ramp anneal from 300 K up to 1500 K
Ultra high vaccum
Temperature of released helium related to the type of trap and thermal stability (He-defect binding energy)
Amount of He released associated with defect concentration

## Slide 9: Experimental details

## Slide 10: Experimental
Eurofer97 - Fe-9Cr-1W-0.2V-0.1Ta-0.1C (wt.%)
Tempered martensitic structure
Ion beam Helium implantation (RT)
    Sample size: 1.2 x 1.2 x 0.05 cm2
Measurements
    Positron annihilation DB
    TDS + in situ DB annealing
Energy | 500 keV | 2 MeV
Doses (He/cm2) | 1 x 1014-1017 | 
Current (nA) | 270 – 280 | 120 - 212
Time (h) | 1 - 15 | 
Dpa | 0.08 – 0.8 | 0.07 – 0.7
Ion range (µm) | ~ 1 | ~ 3
TRIM calculation for 1 x 1015 He/cm2
Schematics of implanted sample
PA
TDS
Positron range

## Slide 11: Experimental Techniques
Thermal desorption spectroscopy
    Annealing from 300 K to 1500 K
    Heating rate of 0.33 K/sec
    Vacuum of 10-8 Torr
Positron Beam Doppler Broadening
    In situ annealing with similar annealing rate to TDS
    Annealing duration of 5 min
    Oven cooling
    Measurement at room temperature

## Slide 12: Results He implantations 500 keV & 2 MeV RT, 1014-1017 He/cm2

## Slide 13: VEP 500 keV and 2 MeV, 1014-17 He/cm2
Positron range
 | Implantation Current (µA) | 
Dose (He/cm2) | 500 keV | 2 MeV
1014 | 0.12 | 0.31
1015 | 0.28 | 0.12
1016 | 0.27 | 0.21
1017 | 1.63 | 2.56

## Slide 14
Annealing study
  Increase of S parameter with increasing dose  Dose effect !!!
  Similar behaviour not only within same implantation energy but also comparing both energies
500 keV
  VEP – decrease of S for 1017 He/cm2
    Not observed in annealing study
VEP - 500 keV and 2 MeV, 1014-17 He/cm2

## Slide 15: TDS – 500 keV & 2 MeV Helium release
Chart: Implantation dose
| 100000000000000 | 1000000000000000 | 1E+16 | 1E+17
500 keV | 1.0755 | 0.79277 | 0.021807 | 0.32291
2 MeV | 0.76121 | 0.24404 | 0.021167 | 0.34689

## Slide 16: TDS – 500 keV & 2 MeV
retention: 25-80%
retention: 2%
retention: 75-110%
retention: 35%

## Slide 17: Interpretation of results Example: 500 KeV, 1016 He/cm2
Below 300 K
  Interstitial He is mobile below RT
300 K
  HELIUM IMPLANTATION
Overnight
bake out

## Slide 18: Interpretation of results 500 KeV, 1016 He/cm2
300 – 600 K
  He in substitutional position
  Vacancy assisted diffusion of He
  Annealing of vacancies and vacancies clusters
1 µm

## Slide 19: Interpretation of results 500 KeV, 1016 He/cm2
600 – 800 K
  Dissociation of overpressured HenVm (n < m) clusters
  Possible re-trapping of He
  Formation of bigger clusters
  Stability of S level mainly due to HeV and stable HenVm pairs
1 µm

## Slide 20: Interpretation of results 500 KeV, 1016 He/cm2
800 – 1200 K
  Ostwald ripening – formation of bubbles
  Increase of S for deeper implantation region
    Smaller diffusion length of He before retraping
  Dissociation of HeV pairs
  Phase transition of Eurofer97 (1160 K)
1 µm

## Slide 21: Interpretation of results 500 KeV, 1016 He/cm2
1200 – 1500 K
  Release of He from bubbles
  Dissociation vs. Migration mechanism
1 µm

## Slide 22: Interpretation of results Overall picture

## Slide 23: Final remarks
Higher implantation dose leads to an increase in the S parameter
    Also observed in the positron annealing study
    Repetition of implantation 500 keV, 1017 He/cm2 necessary
Similar TDS spectra shape for all doses
    Increasing He release up to 1500 K
    Phase transition/HeV dissociation in the range 1100 – 1200 K
    Peak on the left of the phase transition peak
Helium release mechanisms are identified

## Slide 24: Future work
Continuation of He implantations
Desorption experiments
    He implanted samples
    Neutron irradiated samples
TEM
    Neutron irradiated samples
Correlation of microstructure and mechanical properties