## Slide 1: SANS-TEM results correlation on irradiated steels *
R. Coppola1, M. Klimenkov2, R. Lindau2, L. Porcar3, M. Sepielli1, M. Valli4
1 ENEA-Casaccia, Via Anguillarese 301, 00123 Roma, Italy
2 KIT-IAM, PO Box 3640, D- 76021 Karlsruhe, Germany
3ILL, 6, rue Jules Horowitz, 38042 Grenoble, France
4ENEA- Faenza, Via Ravegnana 186, 48018 Faenza (RA), Italy
* based on oral contribution to sas2012 conference, Sydney, November 2012
4th Workshop on Nuclear Fe Alloys
University of Edinburgh, 4th – 5th June 2013

## Slide 2
Current activities
EFDA:
SANS study of neutron irradiated Eurofer97, SANS and high resolution neutron diffraction study of ODS steels for fusion applications (in collaboration with KIT)
IAEA:
CRP on Development, Characterization and Testing of Materials of Relevance to Nuclear Energy Sector Using Neutron Beams (microstructural studies of ODS steels)
CRP on Benchmarking of Structural Materials Pre-selected for Advanced Nuclear Reactors (neutron diffraction and PAS study of model ODS welds)
NeT : Neutron Techniques Standardization for Structural Integrity (JRC Petten)
National Programs:
Preliminary SANS studies of fission steels (EERA JPNM proposal)

## Slide 3
Cold neutron beams for fission and fusion irradiated materials studies
Collimated beams of cold (25 meV) neutrons provide a unique experimental tool for microstructural investigation of irradiated materials:
- They interact via the neutron scattering length parameter b varying randomly with Z and allowing to detect light elements like H (b < 0), He or Li and to distinguish for instance Fe and Cr
- Their absorption coefficient is much lower than for X-rays, allowing to investigate samples as thick as 1 mm or more, which is particularly suited for non-destructive stress investigation of TMB’s and divertor prototypes
Their magnetic moment allows to investigate magnetic materials
No special metallurgical preparation is generally required and sample manipulation is considerably reduced with respect to other techniques, therefore neutron scattering techniques are quite suitable for highly irradiated samples

## Slide 4
SANS instrument D22 at the ILL-Grenoble

## Slide 5
IM + IN
IN
H = 1.4 T
Nuclear and Magnetic SANS
a) reference sample, b) irradiated sample
Nuclear and magnetic SANS cross-section
Polarised SANS

## Slide 6
where B3,N (x) is n-th of N bell-shaped functions defined in a grid of N+3 knots equally distributed in the range Rmin – Rmax, cn> 0 (with the normalisation condition ) and N(R) >0.
No a-priori assumption on N(R), logR representation useful for highly polydispersed systems
N (R) is written as linear combination of N cubic B-splines:
Ref.s:
M. Magnani, P. Puliti, M. Stefanon, Nucl. Inst. Meth. A271 (1988) 611
R. Coppola, R. Kampmann, M. Magnani, P. Staron, Acta Mat. 46 (1998) 5447
B-spline transformation procedure

## Slide 7
Previous work:
  SANS study of fusion martensitic steel implanted with high energy - particles (just helium bubbles to detect…)
This work:
  SANS study of european fusion reference martensitic steel Eurofer97 (0.12 C, 9 Cr, 0.2 V, 1.08 W wt%); original composition modified by alloying natural B contents variable between 10 and 1000 ppm to produce, under neutron irradiation and consequent B activation, corresponding helium bubble distributions.
  B-alloyed Eurofer97 has been neutron irradiated at the HFR of the JRC-Petten for T = 250 °C - 450 °C up do a dose level of 16 dpa (displacement per atom): in this case helium bubbles are produced together with dpa, originating microvoids and changes in precipitate composition.

## Slide 8
He bubbles in F82H-mod. martensitic steel implanted with -particles at 250°C (400 appm), then annealed 2 h at temperatures between 550° C and 975 °C
Coalescence of helium bubbles after annealing at 975 °C
Ref.:
R. Coppola, M. Klimenkov, R. Lindau, A. Möslang, M. Valli, A. Wiedenmann, J. N. M. 409 (2011) 100

## Slide 9
F82H-mod. steel as-implanted at 250°C then tempered at 825° C:
Left - SANS cross-sections of implanted and reference samples
Right - best-fit He bubble volume distributions D(R) (N (R) x V (R)) in Å-1 in compared with the corresponding TEM histogram
Ref:
R. Coppola, M. Klimenkov, M. Magnani, A. Möslang, M. Valli, J. N. M. 329-333 (2004) 1057

## Slide 10
HELIUM BUBBLES VOLUME DISTRIBUTION IN F82H-mod.
IMPLANTED WITH -PARTICLES AT 250 °C
250 °C as–impl.
2 h 825 °C
2 h 975 °C
The dashed area represents the 80% confidence band
Ref.:
R. Coppola, M. Klimenkov, R. Lindau, A. Möslang, M. Valli, A. Wiedenmann, J. N. M. 409 (2011) 100

## Slide 11
Temperature | V | CHe(appm) | RV(Å)
250 °C as-impl. | 0.0012 (0.0039) | 209.0 | 11.1 (7)
825 °C | 0.0053 (0.0036) | 375.9 | 3.8 14.6 (17)
975 °C | 0.0085 (0.0054) | 558.9 | 4.1 45.9 (46)
Best-fit helium bubble volume fraction, V, helium concentration, CHe, and radii obtained from SANS data. The R and V values in parentheses are those obtained from TEM.
Ref.:
R. Coppola, M. Klimenkov, R. Lindau, A. Möslang, M. Valli, A. Wiedenmann, J. N. M. 409 (2011) 100

## Slide 12: Irradiated Structural Material
Chemical compositions of the test alloys in wt.%
Heat | C | Si | Mn | Cr | Mo | Ni | B | V | W | N | Ta | Fe
EUROFER97 | 0.12 | 0.04 | 0.48 | 8.91 | <0.001 | 0.02 | < 0.001 natB | 0.2 | 1.08 | 0.02 | 0.14 | Rest
806 ADS2 | 0.109 | 0.020 | 0.602 | 9.31 | 0.002 | 0.005 | 0.0082 natB | 0.190 | 1.27 | 0.021 | 0.055 | Rest
826 ADS3 | 0.095 | 0.031 | 0.395 | 8.80 | 0.046 | 0.008 | 0.0083 10B | 0.193 | 1.125 | 0.028 | 0.088 | Rest
825 ADS4 | 0.10 | 0.03 | 0.38 | 9.00 | 0.028 | 0.006 | 0.1160 10B | 0.197 | 1.06 | 0.025 | 0.08 | Rest
Heat Treatment: 1040 °C 30 min + 760 °C 90 min
< 10 ppm natB
82 ppm natB
83 ppm 10B
1160 ppm 10B
<10 appm He
~80 appm He
~415 appm He
~5800 appm He
He Concentration
Neutron fluence rate:
1.42x1018 m-2s-1 (thermal);
3.99 x1018 m-2s-1 (fast, >0.1 MeV)
Irradiation HFR-Petten up to 16.3 dpa at T = 250°C, 350°C, 450°C

## Slide 13
Investigation of B doped alloys
He bubbles in ADS3 (450°C), 415 appm He, 16 dpa
Cuboidal helium bubbles decoration of grains boundaries and dislocations lines

## Slide 14
B-alloyed Eurofer97: 400appm He, 16 dpa, 450°C (full dots),
reference (empty dots)
D22, 2 m and 11 m, 6 Å
Nuclear SANS cross-section
Nuclear plus magnetic SANS cross-section

## Slide 15
B-alloyed Eurofer97: 400appm He 16 dpa 450°C (full dots),
reference (empty dots)
Porod check (nuclear component) for 11 m 6 Å: Porod length of ~ 600 Å for M23 C6 precipitates and of ~ 1000 Å for microvoids

## Slide 16
Eurofer97 400appm He 16 dpa 450°C (full dots), reference (empty dots) – Cr-rich carbides in the ref. disappear after irradiation
Eurofer97 400appm, He 16 dpa, 450°C after subtraction of reference – no magnetic contrast, only one type of scatterers
R(Q) behaviour

## Slide 17
B-alloyed Eurofer97 400 appm He 16 dpa 450°C
contrast 0.484 1010 cm -2 for helium bubbles, 7 splines, volume fraction 1.6 %

## Slide 18
B-alloyed Eurofer97 400 appm He 16 dpa 450°C
contrast 0.484 1010 cm -2 for helium bubbles, 5 splines, volume fraction 0.9 %

## Slide 19
TEM – SANS (5 spline) comparison for B-alloyed Eurofer97 400appm He, 16 dpa, 450°C
Size distribution
Volume distribution
Histogram – truncation effects for R < 1 nm

## Slide 20
Distributions obtained from the difference irradiated – reference
(dashed area 80% confidence band)
B-alloyed Eurofer97 400appm He 16 dpa 450°C
contrast 0.484 1010 cm -2 for helium bubbles, 5 splines, volume fraction 0.8 %
The contribution from bubbles with R < 10 Å is almost suppressed
Size distribution
Volume distribution

## Slide 21
TEM histogram and best-fit SANS volume distribution
B-alloyed Eurofer97 400appm He 16 dpa 450°C

## Slide 22
CONCLUSIONS – WORK IN PROGRESS
Appropriate background evaluation gives SANS helium bubble distributions consistent with TEM results, to be further checked by:
- TEM volume fraction determination
- comparison with other SANS transformation methods (eg SASfit)
Q < 10-3 Å-1 and polarized SANS measurements useful to unambiguously identify the large scatters and improve the reliability of the obtained distributions

## Slide 23
ADDITIONAL SLIDES

## Slide 24
R. Coppola, R. Kampmann, M. Magnani, P. Staron, Microstrucural investigation, using polarized neutron scattering, of a martensitic steel for fusion reactors, Acta mat. 46 (1998) 5447
R. Coppola, C. D. Dewhurst, R. Lindau, R. P. May, A. Möslang, M. Valli, Polarised SANS study of microstructural evolution under neutron irradiation in a martensitic steel for fusion reactors, Physica B 345 (2004) 225
R. Coppola, M. Klimiankou, R. Lindau, A. Möslang, M. Valli, Helium-bubble evolution in F82H mod – Correlation between SANS and TEM, J. N. M. 329-333 (2004) 1057
R. Coppola, R. Lindau, M. Magnani, r. P. May, A. Möslang, J. W. Rensman, B. van der Schaaf, M. Valli, Microstructural investigation, using SANS, of neutron irradiated Eurofer97 steel, F. Eng. & Des. 75-79 (2005) 985
R. Coppola, R. Lindau, R. P. May, A. Möslang, M. Valli, Investigation of microstructural evolution under neutron irradiation in Eurofer97 steel by means of small-angle neutron scattering, J. Nucl. Mat. 386-388 (2009) 195-198
R. Coppola, R. Lindau, A. Möslang, M. Valli, A. Wiedenmann, Recent applications of small-angle neutron scattering in the characterisation of irradiated steels for nuclear technology, pres. at EC-IAEA Workshop, Barcelona October 2009 J. Nucl. Mat. 409 (2011) 100
REFERENCES

## Slide 25
SANS contrast depends on bubble radius R
The dependence of the contrast on the bubble radius is taken into account in the fitting procedure but given the small value of rHe very large changes of the He mass density would be necessary to lead to significantly different distributions. Assuming that the He concentration is equal to the nominal value (400 appm), the obtained variations on range typically from –10% at 2 Å to +12% at 100 Å. The resulting variations in N(R) are generally of a few per cent, therefore well inside the statistical uncertainty band
D r (R) = rF82H – bHerHe(R)

## Slide 26
Nuclear SANS cross-sections of the difference between Eurofer97 neutron irradiated at 250°C at 2.5 dpa and at 300°C at 8.4 dpa and their respective reference samples
RESULTS ON 2.5 AND 8.4 dpa IRRADIATED EUROFER
8.4 dpa
2.5 dpa

## Slide 27
Increasing the dose the average radius remains nearly unchanged but a consistent increase is observed in the volume fraction of the observed defects, from 0.005 at 2.5 dpa to 0.011 at 8.4 dpa
MICROVOIDS EVOLUTION WITH IRRADIATION DOSE
Volume distribution functions D(R) (nm-1) obtained from the nuclear SANS difference between Eurofer97 neutron irradiated at 300°C and their respective reference samples (R. Coppola et al. J. Nuc. Mat. 386-388 (2009) 195)
8.4 dpa
2.5 dpa

## Slide 28
B-alloyed Eurofer97 400appm He, 16 dpa, 450°C
(after subtraction of reference, un-irradiated sample)
Nuclear
Nuclear plus magnetic