## Slide 1: Diffusion of point defects and SIA clusters in dilute Fe-Ni alloys
A.Serra1, N.Anento1, D.Terentyev2 & Y.N.Osetsky3
1.Universitat Politècnica de Catalunya (UPC), Spain
2. Institute of Nuclear Materials Science (SCK-CEN), Belgium
3. Oak Ridge National Laboratory, TN, USA
(EU Project PERFORM60)

## Slide 2: Motivation
Experimental evidence *: Addition of Ni promotes nucleation and/or immobilization of SIA clusters and small dislocation loops.
  %Ni↑: Size ↓, density↑, relative fraction of a/2<111> loops↑
‘Loop stabilization' effect leads to reduction of the void growth since homogenously distributed small (TEM invisible) loops act as efficient sinks for vacancies
*(Mat.Res.Soc. Symp. Proc., 373 (1995) 57; PERFECT_Report:D1-3.8)
How Ni solid solution affects the mobility of in-cascade generated SIA clusters in dilute Fe-Ni alloys

## Slide 3: Outline
Point defects (PD)
  PD - Ni Interaction energy
  PD diffusion in Fe and Fe-Ni
SIA clusters (7, 19 & 37) (Radius < 1nm)
  Cluster – Ni Interaction energy
  Cluster diffusion in Fe-0.8%Ni

## Slide 4: Vacancy migration energy barrier and Vac-Ni Binding energy
Em(Fe) | 0.63
Em(Ni) | 0.61
Em(Fe, Ni 2nn) | 0.52
Em(Fe, Ni 3nn) | 0.71
Em(Fe, Ni 5nn) | 0.68
Eb(1nn) | -0.02
Eb(2nn) | 0.10
Vacancy migration energy barrier (eV) *
Ni-Vacancy binding energy (eV) *
Fe diffusion coefficients (m2/s)
Ea =0.56eV
*Interatomic potential Fe-Ni: G. Bonny et al. MSMS Eng. 17 (2009) 025010

## Slide 5: Vacancy diffusion in Fe-0.8%Ni
1400 1000 800 600
T (K)

## Slide 6: SIA migration and SIA-Ni E
EmFe-Fe (bulk) | 0.31
EmFe-Fe Ni(1nn) tens. | 0.35
EmFe-Fe Ni(1nn) comp. | 0.23
Single SIA migration energy barrier (eV)
EbFe-Fe Ni(1nn) tens. | -0.14
EbFe-Fe Ni(1nn) comp. | -0.12
EbFe-Ni Ni(1nn) comp. | -0.35
Ni-SIA binding energy (eV)*
Matrix atom
Solute atom
Fe-Fe <110> Ni (1nn) tension
Fe-Fe <110> Ni (1nn) compression
Fe-Ni <110> Ni (1nn) compression
*G. Bonny et al. MSMS Eng. 17 (2009) 025010

## Slide 7: 1 SIA (0.5 to 1.6%Ni)
Ea (Fe)= 0.27eV
Ea (Ni)= 0.32eV

## Slide 8: Ni-Cluster binding energy
17
61SIAs
Eb (centre)= 0.07 eV
Eb (edge) = 0.26eV
7SIAs
Eb (centre)= 0.15 eV
Eb (edge) = 0.22eV

## Slide 9: 7SIAs
[111]
[1-10]
900K 600K 450K

## Slide 10: 19SIA cluster
900K 600K 450K 300K

## Slide 11: 37SIAs
500K
900 600 500 450 300
T (K)

## Slide 12: Cluster diffusion @ Fe-0.8%Ni
900 600 500 450 400 300
T (K)

## Slide 13: Summary
We studied diffusion of point defects and SIA clusters in dilute Fe-Ni alloys (0.5, 0.8, 1.6 wt%Ni)
Diffusion of point defects is almost not affected by Ni solid solutions from 0.5 to 1.6%
The mobility of SIA clusters is strongly affected by Ni and decreases with size of cluster and concentration of Ni
Ni in low concentrations provides the necessary friction to slow down clusters decreasing the diffusion coefficient and increasing the activation energy

## Slide 15: Defect diffusivity vs. temperature
Defect diffusion coefficient calculation:
TTD: Time trajectory decomposition
SD: Self diffusion coefficient
JFA: Jump Frequency Analysis
n: dimensionality of diffusion
Nsd: number of isochronal segments of tsd.
Em: migration energy
D=D0 exp(-Em/KT)